Hauthaway                                  				   Established 1852

C. L. Hauthaway & Sons Corporation                                                                  781 592-6444

638 Summer Street   Lynn, MA  01905-2092                                          	    www.hauthaway.com

Hauthane HD-2142 DMM

DESCRIPTION:		An NMP-free, APEO-free, aliphatic, polyester-based, water-borne polyurethane dispersion.

SUGGESTED USES:	HD-2142 DMM was developed for use on flexible and rigid PVC, and treated polypropylene film.  Coatings containing this polymer form hard, tough, hydrolysis-, chemical- and stain-resistant films.  Superior adhesion to PVC makes it the ideal candidate for vinyl sheet goods, automotive interior parts, vinyl furniture and components.

CHARACTERISTICS:	•	Superior adhesion to PVC and treated polypropylene film

•	Excellent UV resistance

•	Exceptional alcohol resistance

•	Humidity resistance

•	Contains dipropylene glycol dimethyl ether (DMM) co-solvent

APPLICATION:		HD-2142 DMM may be used as a sole vehicle or blended with acrylic emulsions. Viscosity modification can be made with associative thickeners for application via spray, knife-over-roll, or other methods.

DRYING:			The addition of coalescing solvent is recommended to achieve optimal film formation with HD-2142 DMM.  In ambient-cured systems the addition of  5-10% DPnB coalescing solvent is suggested.  Less coalescing solvent is required in heat-cured systems to attain comparable film properties.   Typical oven drying temperatures and dwell times for aqueous coatings are sufficient to produce optimal film properties.

PHYSICAL PROPERTIES						TENSILE PROPERTIES

SOLIDS			35% (±1%)				(TESTED AT 2 INCHES/MINUTE)

VISCOSITY		   	50-1000 cps				ELONGATION	  	   185 %

DENSITY	  		1.05 kg/l					TENSILE STRENGTH	     31 MPa

pH				7.5 - 10.0				100% MODULUS	     24 MPa

SOFTENING POINT		NA					200% MODULUS	   NM

VOC CONTENT		91 g/l (as supplied)		300% MODULUS	   NM

# HD-2142 DMMcl-EC												Revised 6/21