Hauthaway                                  					 Established 1852

C. L. Hauthaway & Sons Corporation                                                         	  	    781 592-6444

638 Summer Street   Lynn, MA  01905-2092                                          		  www.hauthaway.com

Hauthane HD-2139

DESCRIPTION:		An aliphatic, polyester-based, aqueous urethane dispersion specifically developed for factory coated PVC flooring.

SUGGESTED USES:	HD-2139 was developed as a high gloss, no wax topcoat for expanded PVC flooring.  Can be factory applied as a fused coating during PVC expansion.  HD-2139 is ideally suited for PVC roll or sheet goods requiring a 180 degree reverse bend.

CHARACTERISTICS:		High gloss

- Excellent mar and wear resistance

- Excellent resistance to staining

- Remarkably high balance of physical properties

- Contains n-methyl pyrrolidone (NMP) co-solvent

APPLICATION:		HD-2139 can be used as a sole vehicle or blended with acrylic emulsions and applied by rotogravure, reverse roll, flexible blade, or wire wound rod.  It may be thickened for alternative application methods.

CURING:			HD-2139 should be dried by forced hot air or heat lamp before entering oven.  Typical drying temperatures and dwell times for aqueous coatings are sufficient to produce optimal film properties. Maximum performance is attained with additions by weight of 5% HA-801 melamine crosslinker or 4% HA-800 aziridine crosslinker.

PHYSICAL PROPERTIES				TENSILE PROPERTIES

SOLIDS		33% (± 1%)				 (Tested at 2 inches/minute)

VISCOSITY		50-150 cps				ELONGATION		    135%

pH			7.0-9.5					TENSILE STRENGTH	>6000 psi

DENSITY		8.7 lbs/gal				100% MODULUS	  5700 psi

SOFTENING POINT	360°F					200% MODULUS	     NA

VOC CONTENT	122 gm/l					300% MODULUS	     NA

SWARD HARDNESS	50

HD-2139cl 	Revised 5/04