Hauthaway                                  				   Established 1852

C. L. Hauthaway & Sons Corporation                                                        	       781 592-6444

638 Summer Street   Lynn, MA  01905-2092                                          	     www.hauthaway.com

Hauthane L-3528

DESCRIPTION:		A co-solvent free, polycarbonate-based, aliphatic, polyurethane dispersion.

SUGGESTED USES:	L-3528 was developed for general coatings use on wood, plastic and metal substrates.  The product offers exceptional resistance to hydrolysis, oxidation and UV-degradation.  L-3528 is ideally suited for exterior applications where film durability and longevity are important considerations.

CHARACTERISTICS:	<	Excellent exterior weathering durability

<	Excellent humidity resistance

          Outstanding toughness and abrasion-resistance

<	Co-solvent free, tin-free, APEO-free

APPLICATION:		L-3528 may be formulated into coatings applied by spray, brush or pad applicator.  It can be used as a sole vehicle or blended with acrylic emulsions. The rheology may be modified with associative thickeners.

CURING:		            L-3528 may be air dried, if desired, depending on film thickness.  The addition of 5 – 10% coalescing solvent is suggested in ambient temperature drying situations.  Typical oven drying temperatures and dwell times for aqueous coatings may be sufficient to produce optimal film properties.

PHYSICAL PROPERTIES					TENSILE PROPERTIES

SOLIDS		35 (±1%)				(TESTED AT 20 INCHES/MINUTE)

VISCOSITY		50-500 cps				ELONGATION		  340 %

DENSITY  		1.06					TENSILE STRENGH	4400 psi

pH			7.5 - 10.0				100% MODULUS	2040 psi

VOC CONTENT	12 g/l (as supplied))			200% MODULUS	2700 psi

VOC CONTENT	41 g/l (less water)		            	300% MODULUS	3800 psi

SOFTENING POINT	380°F

SWARD HARDNESS	41

# L-3528cl													Revised 2/19