Hauthaway                                  					Established 1852

C. L. Hauthaway & Sons Corporation                                                         	  	  781 592-6444

638 Summer Street   Lynn, MA  01905-2092                                          		 www.hauthaway.com

Hauthane L-3529

DESCRIPTION:		A solvent free, flexible, aliphatic, polycarbonate polyurethane dispersion.

SUGGESTED USES:	L-3529 was designed primarily for use on flexible substrates as a coating, saturant or impregnant.  It may be blended with L-3528 to increase hardness.

CHARACTERISTICS:               Maximum hydrolytic stability and oxidation resistance

         Outstanding toughness and abrasion resistance

- Good water and chemical resistance

- Can be crosslinked to enhance performance

- Solvent free, Tin free, APEO free.

APPLICATION:		L-3529 can be used as a sole vehicle or blended with acrylic emulsions for spray or rotogravure applications.  It may be thickened with associative thickeners for knife-over-roll or similar methods.

DRYING:			L-3529 may be air dried, if desired, depending on film thickness. Typical drying temperatures and dwell times for aqueous coatings are sufficient to produce optimal film properties.

PHYSICAL PROPERTIES				TENSILE PROPERTIES

SOLIDS		35% (±1%)			 (Tested at 20 inches/minute)

VISCOSITY		75-200 cps			ELONGATION		    640 %

pH			8.5-10.0				TENSILE STRENGTH	  3650 psi

DENSITY		8.8 lbs/gal			100% MODULUS	    375 psi

VOC CONTENT	35 g/l (less water)			200% MODULUS	    545 psi

SOFTENING POINT	300°F				300% MODULUS	    800 psi

SWARD HARDNESS	10

L-3529cl 												Revised 2/19