Hauthaway                                  				   Established 1852

C. L. Hauthaway & Sons Corporation                                                         	       781 592-6444

638 Summer Street   Lynn, MA  01905-2092                                          	     www.hauthaway.com

Hauthane HD-6000 DMM

DESCRIPTION:		An NMP-free, APEO-free, polyester-based, hydroxyl-functional, aliphatic, water-borne polyurethane dispersion.

SUGGESTED USES:	HD-6000 DMM was developed for use with water-dispersible, isocyanate crosslinkers such as Covestro’s Bayhydur 302 or Vencorex’s Easaqua X D 401.  The product, when crosslinked provides tough, chemical-resistant, semi-gloss coatings which may be applied to a variety of substrates including concrete, metals, plastics and wood materials.

CHARACTERISTICS:		Superior chemical resistance

<	Excellent exterior weathering durability

<	Excellent humidity resistance

<	Contains dipropylene glycol dimethylether co-solvent

APPLICATION:		HD-6000 DMM crosslinked with water-dispersible isocyanates may be spray applied using single-component equipment.  The workable potlife is approximately 3 hours at the suggested crosslinker ratio of 2.0 to 1.0 NCO / OH.

CURING:			HD-6000 DMM, crosslinked with a water dispersible isocyanate, will dry to a hard film in 30 minutes at ambient room temperature (65 – 70(F) and humidity (RH 50%).  Ultimate cured properties will take 3 -5 days to develop.  If heat is available, the ultimate properties can be attained in shorter time.  Typical oven drying temperatures and dwell times for aqueous coatings are sufficient to produce optimal film properties.

PHYSICAL PROPERTIES						TENSILE PROPERTIES

SOLIDS			35 (± 1%)				(TESTED AT 20 INCHES/MINUTE)

VISCOSITY			50-500 cps				ELONGATION		   230 %

DENSITY			8.8 lbs/gal				TENSILE STRENGTH	 7000 psi

pH				7.5 - 10.0				100% MODULUS	 4850 psi

VOC CONTENT		70 g/l (as supplied)		200% MODULUS	 6800 psi

OH EQUIVALENT WT.		3,100 (as supplied)		300% MODULUS	   NM

SWARD HARDNESS		44

# HD-6000 DMMcl												Revised 6/21